|  |  |  |
| --- | --- | --- |
| **BIRCOcanal NW 500 – Supply channels with angles** with integrated two-sided anchoring system (AS) made of concrete+ External width at angle 650, at ground 690 mm+ Internal width 500 mm+ External construction height 550 mm, internal height 415 mmmade of concrete C 40/50, CE compliance with EN 1433, up to load class F 900 as defined by EN 1433, with anchored 4 mm hot-dipped galvanized solid steel angles for combi-closure system (70 µm zinc coating), with safety sealing joint[ ] \_\_\_\_\_ m BIRCOcanal NW 500 AS channel length 1000 mm, with cast-in mounting rails[ ] \_\_\_\_\_ m BIRCOcanal NW 500 AS channel length 1000 mm, without mounting rails[ ] Sealing with SF-Connectincluding the necessary end caps, delivery and installation according to manufacturer’s installation instructions.Manufacturer: BIRCO GmbHHerrenpfädel 142, D 76532 Baden-BadenPhone +497221 - 5003-0; Fax +497221 - 5003-1219; www.birco.de | **Unit price** | **Total price** |
| **BIRCOcanal NW 500 AS – Gratings for supply channels with angles**+ Width 633 mm+ Height 45 mmload class according to DIN EN 1433, with 8 point per metre M16/A2-bolt fastening or Easylock fastening[ ] \_\_\_\_\_ pce bulb ductile iron cover(s) black immersion- lacquered, length 500 mm, load class E 600delivery and installation according to manufacturer’s installation instructions.Manufacturer:BIRCO GmbH | **Unit price** | **Total price** |

|  |  |  |
| --- | --- | --- |
| **BIRCOcanal NW 500 AS – Supply channels without angles** with integrated two-sided anchoring system (AS) made of concrete+ External width 650 mm, internal width 690 mm+ External construction height 500 mm, internal height 410 mmmade of concrete C 40/50, CE compliance with EN 1433, up to load class F 900 as defined by EN 1433, with safety sealing joint[ ] \_\_\_\_\_ m BIRCOcanal NW 500 AS channel length 1000 mm  with cast-in mounting rails[ ] \_\_\_\_\_ m BIRCOcanal NW 500 AS channel length 1000 mm  without mounting rails[ ] Sealing with SF-Connectdelivery and installation according to manufacturer’s installation instructions.Manufacturer: BIRCO GmbHHerrenpfädel 142, D 76532 Baden-BadenPhone +497221 - 5003-0; Fax +497221 - 5003-1219; www.birco.de | **Unit price** | **Total price** |
| **BIRCOcanal NW 500 AS – Covers for supply channels without angles**+ Smoothed surface[ ] \_\_\_\_\_ pce concrete cover length 5000 mm  until 1 m height above ground[ ] \_\_\_\_\_ pce reinforced concrete cover length 1000 mm load class SLW 60delivery and installation according to manufacturer’s installation instructions.Manufacturer:BIRCO GmbH | **Unit price** | **Total price** |
| **BIRCOcanal NW 500 AS – Drilled hole in channel base**[ ] \_\_\_\_\_ in horizontal / vertical direction, diameter DN 300Delivery.Manufacturer:BIRCO GmbH | **Unit price** | **Total price** |